## Slide 1: The Development of Large-Area Pico-second Photodetectors
Henry Frisch, Enrico Fermi Institute, Univ. of Chicago
For the LAPPD Collaboration

## Slide 2: Outline
Motivation(s) and Applications
LAPPD
Micro Channel Plates
Hermetic Packaging, signal and HV circuits
Electronics and DAQ (plug-and-play)
Photocathodes
Results
Opportunities and Challenges
Acknowledgements- LAPPD collaborators, Howard Nicholson and the DOE HEP, ANL Management, and the NSF.

## Slide 3: Motivation

## Slide 4: Colliders:
Approach: measure the difference in arrival times of photons and charged particles which arrive a few psec later.
Light source is Cherenkov light in the window/radiator.
Benefit: Discoveries in signatures not possible now
Need: 1) identify the quark content of charged particles
2) vertex photons
(Note: conventional TOF resolution is 100 psec -factor of 100 worse than our goal= 1” is 100 psec, so need a small scale-length).
Extract all the information in each event (4-vectors) – only spins remain…

## Slide 5
Need, e.g.- Higgs to gamma-gamma at the LHC - tie the photons to the correct vertex, and more precisely reconstruct the mass of the pair
Major problem coming up at LHC- vertexing at high luminosity (e.g. Joe Incandela’s UC seminar on CMS)
Time (ns)
Vertex position along beam line (cm)
3 different interactions in one beam crossing
Multi-vertex event at CDF (Tevatron)

## Slide 6: Neutrino Physics
Approach: measure the arrival times and positions of photons and reconstruct tracks in water
Benefit: Factor of 5 less volume needed, cost.
Need: lower the cost and extend the reach of large neutrino detectors
Competition- large PMT’s, Liquid Argon
H. Nicholson

## Slide 7: Can we build a photon TPC?
Work of Matt Wetstein (Argonne,&Chicago) in his spare time (sic)

## Slide 8: Matt Wetstein; ANL&UC
Works on GEANT events too

## Slide 9: Daniel Boone
Proposal (LDRD) to build a little proto-type to test photon-TPC ideas and as a simulation testbed
`Book-on-end’ geometry- long, higher than wide
Close to 100% coverage so bigger Fid/Tot volume
Dx, Dy << 1 cm
Dt < 100 psec
Magnetic field in volume
Idea: to reconstruct vertices, tracks, events as in a TPC (or, as in LiA).
n
2 m
2 m
1 m
caps
Daniel
Also ANNIE- Bob Svoboda

## Slide 10
(T1, X1, Y1 )
(T2, X2, Y2 )
Vertex (e.g. p0->gg)
Tv, Xv, Yv, Zv
Photon 1
Photon 2
Detector Plane
One can reconstruct the vertex from the times and positions- 3D reconstruction
(t1-tv)c
(t2-tv)c
Rare Kaon Decays- backgd rejection by reconstructing p0 vertex space point:
E.g. for KOTO (Yau Wah, JPARC)-beat down combinatoric p0 bkgds

## Slide 11: Good timing alone doesn’t do it-
The ALICE TPC:
Drift electrons onto wires that measure where and when for each electron.
Good time resolution would buy nothing if one integrated over a whole (blue) TPC sector- ie didn’t correlate when and where
when and where
Correlated time and space points allow 3D reconstructions

## Slide 12: Medical Imaging (PET)
Need: 1) much lower dose rate
2) faster through-put
3) real-time feedback (therapy as well as diagnosis)
Approach: precise Time-of-Flight, sampling, real-time adaptive algorithms in local distributed computing, use much larger fraction of events and information
Benefit: higher resolution, lower dose to patient, less tracer production and distribution, new hadron therapy capabilities
Competition: Silicon PMT’s

## Slide 13: Sampling Calorimetry in PET?
Depth in crystal by time-difference
Heejong Kim
Heejong Kim
Can we solve the depth-of-interaction problem and also use cheaper faster radiators?
Alternating radiator and cheap 30-50 psec planar mcp-pmt’s on each side
Depth in crystal by energy- asymmetry
Simulations by Heejong Kim (Chicago)

## Slide 14: An Energy-Flow MCP-based Calorimeter?
Electron pattern (not a picture of the plate!)- SSL test, Incom substrate, Arradiance ALD. Note you can see the multi’s in both plates => ~50 micron resolution
Note- at high gain the boundaries of the multi’s go away
Pores saturate => output is proportional to number of pores.?Transmission line readout gives a cheap way to sample the whole plane with pulse height and time- get energy flow.
Oswald Siegmund, Jason McPhate, Sharon Jelinsky, SSL (UCB)

## Slide 15: Cherenkov-sensitive Sampling Quasi- Digital EM/Had-separating Calorimeters
A picture of an em shower in a cloud-chamber with ½” Pb plates (Rossi, p215- from CY Chao)
A `cartoon’ of a fixed target geometry such as for JPARC’s KL-> pizero nunubar (at UC, Yao Wah) or LHCb

## Slide 16: Cherenkov-sensitive Sampling Quasi- Digital Calorimeters
A picture of an em shower in a cloud-chamber with ½” Pb plates (Rossi, p215- from CY Chao)
A `cartoon’ of a fixed target geometry such as for JPARC’s KL-> pizero nunubar (at UC, Yao Wah) or LHCb

## Slide 17: LAPPD

## Slide 18: The 4 `Divisions’ of glass LAPPD
CV
CV
Hermetic Packaging
CV
CV
Electronics/Integration
MicroChannel Plates
Photocathodes

## Slide 19: “Portfolio of Risk- Parallel Efforts
Two parallel but intertwined efforts at different levels of risk, reward:
  SSL/Hawaii (Siegmund)- ceramic package based on Planacon experience, NaKSb cathode, higher cost, smaller area, lower throughput, lower risk due to fewer innovations, more experience;
  ANL/UC (Wagner, Byrum,Frisch)- glass package, KCsSb cathode, lower cost, larger area, higher throughput, higher risk, but more innovation and use of new technologies.
Reduce risk and enhance reward by diversification onto the 2 paths. Has proved very beneficial to both efforts (much cross-fertilization, and shared MCP development)

## Slide 20: Parallel Efforts on Specific Applications
.
LAPD Detector Development
PET
(UC/BSD, UCB, Lyon)
Collider
(UC, ANL,Saclay.
Mass Spec
Andy Davis, Mike Pellin, Eric Oberla
Non-proliferation
LLNL,ANL,UC
Drawing Not To Scale (!)
ANL,Arradiance,Chicago,Fermilab, Hawaii,Muons,Inc,SLAC,SSL/UCB, UIUC, Wash. U
Explicit strategy for staying on task-
Multiple parallel cooperative efforts
All these need work- naturally tend to lag the reality of the detector development
Neutrinos
(Matt, Mayly, Bob, John, ..; Zelimir)
Muon Cooling
Muons,Inc
(SBIR)
K->pnn
JPARC

## Slide 21: MCP’s

## Slide 22: How Does it Work?
Requires large-area, gain > 107, low noise, low-power, long life, 
(t)<10 psec, (x) < 1mm, and low large-area system cost
Realized that an MCP-PMT has all these but large-area, low-cost:
(since intrinsic time and space scales are set by the pore sizes- 2-20µ)
window
Photocathode on inside of window
Pair of micro-channel plates
RF strip-line anode
Incoming charged particle
Photo-electron
from cathode
Radiated Cherenkov photon
Output pulse of 107 electrons

## Slide 23: So what are the new technologies?
Glass capillary substrates (Incom)
Atomic Layer Deposition (Arradiance, ANL)
RF transmission line anodes (Tang, UC..)
Waveform Sampling (Hawaii, MPI, Orsay,Saclay, UC)
Cheap plate glass, frit seals, silk-screened anodes, home-brew indium seals, …
However- there are areas where we have only old technologies and need new ones-
Challenges and opportunities (have some fun while you’re mostly typing in deathless C++)

## Slide 24: Simplifying MCP Construction
Chemically produced and treated Pb-glass does 3-functions:
Provide pores
Resistive layer supplies electric field in the pore
Pb-oxide layer provides secondary electron emission
Conventional Pb-glass MCP
OLD
Incom Glass Substrate
NEW
Separate the three functions:
Hard glass substrate provides pores;
Tuned Resistive Layer (ALD) provides current for electric field (possible NTC?);
Specific Emitting layer provides SEE

## Slide 25: Micro-Channel Plate Development
Simulation of electric field in 1 or several pores- with endspoiling; (attempted) comparison with data
Incom 8”-sq high-quality MCP plate with > 65% OAR

## Slide 26: Latest Incom Micropore Substrate
.075”
~150 20m pores
INCOM glass substrate
Incom.inc, Charlton Mass
80 million 20-micron pores in an 8”-sq plate
65% open-area ratio; 1.2mm thick (L/D=60)

## Slide 27: Why has 100 psec been the # for 60 yrs?
Typical path lengths for light and electrons are set by physical dimensions of the light collection and amplifying device.
These are on the order of an inch. One inch is 100 psec. That’s what we measure- no surprise! (pictures from T. Credo)
Typical Light Source (With Bounces)
Typical Detection Device (With Long Path Lengths)

## Slide 28: New MCP Structure (not to scale)
28
resistive coating (ALD)
emissive coating (ALD)
conductive coating (thermal evaporation or sputtering)
pore
1 KV
Jeff Elam
Notes: Very schematic – not correct open area ratio
Might need to do Au before Al2O3 for better contact
Add HV leads
28

## Slide 29: Atomic Layer Deposition (ALD) Thin Film Coating Technology
Atomic level thickness control
Deposit nearly any material
Precise coatings on 3-D objects (JE)
Jeff Elam pictures
Lots of possible materials => much room for higher performance
Notes: 29
For the technologies that I’ll be describing today, ALD has attributes that uniquely suit it

## Slide 30
Slade Jokela (ANL)

## Slide 31: ALD &Integration tests at ANL
Argonne Atomic Layer Deposition and Test Facilities
In situ measurements of R (Anil)
Femto-second laser time/position measurements (Matt, Bernhard, Andrey, Razib, Sasha, Bob, Eric)
33 mm development program
8” anode injection measurements
Anil Mani and Bob Wagner
31

## Slide 32: SSL (Berkeley) Test/Fab Facilities
Ossy Siegmund, Jason McPhate, Sharon Jelenski, and Anton Tremsin-
Decades of experience
(some of us have decades of inexperience?)

## Slide 33: Microchannel Plates-4b
Noise (bkgd rate).
<=0.1 counts/cm2/sec; factors of few > cosmics (!)
Ossy Siegmund, Jason McPhate, Sharon Jelinsky, SSL/UCB
Performance:

## Slide 34: Microchannel Plates-4d
Performance: burn-in (aka `scrub’)
Measurements by
Ossy Siegmund,
Jason McPhate,
Sharon Jelinsky, SSL/UCB
Typical MCP behavior- long scrub-times
Measured ANL ALD-MCP behavior
(ALD by Anil Mane, Jeff Elam, ANL)
(Big deal commercially?)

## Slide 35: Signal- want large for S/N
We see gains > 107 in a chevron-pair
Ossy Siegmund, Jason McPhate, Sharon Jelinsky, SSL/UCB
ALD by Anil Mane and Jeff Elam, ANL

## Slide 36: Hermetic Packaging
Internal HV circuit, capacitively coupled signal circuit (no penetrations through glass)- the `frugal tile’

## Slide 37: Tile-Tray Integrated Design
Because this is an RF-based readout system, the geometry and packaging are an integral part of the electronic design
The design is modular, with 8”-square MCP sealed vacuum tubes (`tiles’) with internal strip-lines capacitively coupled to a ground plane (tray) that also holds the electronics.

## Slide 38: The Half-Meter-Squared SuperModule
A `tile’ is a sealed vacuum-tube with cathode, 2 MCP’s, RF-strip anode, and internal voltage divider
HV string is made with ALD
A `tray’ holds 12 tiles in 3 tile-rows
15 waveform sampling ASICS on each
end of the tray digitize 90 strips
2 layers of local processing (Altera)
measure extract charge, time,
position, goodness-of-fit

## Slide 39: SuperModule Mockup: ½-m2 of cathode
Real 8” glass tile package parts- anode, side-wall, window (sic)
`Innards’ stack of 2 MCP’s +3 spacers+anode+window under test
Have read out through from AC card through full DAQ chain to PC

## Slide 40: Demonstration of the Internal ALD HV Divider in the Demountable Tile
Demountable at APS
Scanning the laser: t vs x
Average pulse shape vs HV
IV Curve (expected 32 Megs)

## Slide 41: Electronics and DAQ
The plug-and-play goal for the supermodule

## Slide 42: Extract time, position of pulse using time from both ends
Eric Oberla slide from ANT11

## Slide 43: Developing and Testing the Electronics, Anodes, and DAQ
Eric Oberla (grad student) and Craig Harabedian (engineer) working on the Tray layout and cabling

## Slide 44: Analog Card to Digital Card
Can be direct connection (shown) or cable

## Slide 45: Digital Cards and Central Card
Present readout to PC and Nvidia GPU is via USB;
Ethernet hardware is on boards- later

## Slide 46: Anode Testing for ABW, Crosstalk,..
Network Analyzer Tile Anode
Herve’ Grabas, Razib Obaid, Dave McGinnis

## Slide 47: Anode Testing for ABW, Crosstalk,..
Razib Obaid
Crosstalk
ABW

## Slide 48: Simulation of Resolution vs abw
Jean-Francois Genat (NIM)
Brown line: 10 Gs/sec (we’ve done >15);
1.5 GHz abw ( we’ve done 1.6); S/N 120 (N=0.75mv, S is app specific)
This (brown) line
This (brown) line
1 ps

## Slide 49: The PSEC4 Waveform Sampling ASIC
PSEC4: Eric Oberla and Herve Grabas; and friends…
Eric Oberla, ANT11

## Slide 50
PSEC-4 ASIC
6-channel “oscilloscope on a chip” (1.6 GHz,10-15 GS/s)
Evaluation board uses USB 2.0 interface + PC data acquisition software
LAPPD Collaboration
Eric Oberla, ANT11

## Slide 51: 6-channel `Scope-on-a-chip’
20 GS/scope
4-channels (142K$)
17 GS/PSEC-4 chip
6-channels ($130 ?!)
Real digitized traces from anode
Designed by Eric Oberla (UC grad student)
working in EDG
with EDG tools and engineers
(H. Grabas, J.F. Genat)

## Slide 52
PSEC-4 Performance
Digitized Waveforms
Input: 800MHz, 300 mVpp sine
Sampling rate : 10 GSa/s
Sampling rate : 13.3 GSa/s
Only simple pedestal correction to data
As the sampling rate-to-input frequency ratio decreases, the need for time-base calibration becomes more apparent (depending on necessary timing resolution)
Eric Oberla, ANT11

## Slide 53: Digitization Analog Bandwith
ABW~1.6GHz
3 db loss
PSEC4: Eric Oberla and Herve Grabas+ friends…
Eric Oberla, ANT11

## Slide 54: Noise (unshielded)
PSEC4: Eric Oberla and Herve Grabas+ friends…
RMS=755 microvolts
Full-Scale ~1.2 volts (expect S/N>=100, conservatively)
Eric Oberla, ANT11

## Slide 55: Photocathodes
oy- chemistry…

## Slide 56: Photocathodes
LAPPD goal- 20-25% QE, 8”-square- conv. alkali
2 parallel efforts: SSL (knows how), and ANL (learning)
ANL
Optical stand
First cathodes made at ANL
Burle commercial
equipment

## Slide 57: Status of PhotoCathodes
Have made >20% 8”PC at SSL; 25% small PC’s at ANL, 18% 4” (larger underway)
SSL 8” SbNaK cathode
4” cathode: Chalice in Burle oven
QE of SSL 8” SbNaK cathode
QE of ANL small SbKCs cathodes
ANL
ANL

## Slide 58: Results and Summary

## Slide 59: Internal ALD HV Divider Scheme works
Coat MCP’s and spacers with ALD to form a completely internal resistive divider string-no pins
Anil Mane, Jeff Elam (ANL/ESD)
I-V Curves for the stack
Resistances and voltages for the stack

## Slide 60: Microchannel Plates- lownoise
Noise (bkgd rate).
<=0.1 counts/cm2/sec; factors of few > cosmics (!)
Ossy Siegmund, Jason McPhate, Sharon Jelinsky, SSL/UCB
Performance:

## Slide 61: Microchannel Plates- no aging
Performance: burn-in (aka `scrub’)
Measurements by
Ossy Siegmund,
Jason McPhate,
Sharon Jelinsky, SSL/UCB
Typical MCP behavior- long scrub-times
Measured ANL ALD-MCP behavior
(ALD by Anil Mane, Jeff Elam, ANL)
(Big deal commercially?)

## Slide 62: Microchannel Plates- high gain
We see gains > 107 in a chevron-pair
Ossy Siegmund, Jason McPhate, Sharon Jelinsky, SSL/UCB
ALD by Anil Mane and Jeff Elam, ANL

## Slide 63: 8”-MCP Pair and Strip Anode Work
Laser mirrors and 8” anode for 8” MCP tests
Pulses from one strip of 8” anode with 8” MCP pair
Matt Wetstein, Bernhard Adams, Andrey Elagin, Razib Obaid, Sasha Vostrikov, Bob Wagner

## Slide 64: Timing res agrees with MC
Time resolution on 2 ends of 8”-anode strip vs (S/N)-1 in psec (pair of 8” MCP’s)
< 6 psec
M. Wetstein, B. Adams, A. Elagin, R. Obaid, A. Vostrikov, …
Laser spot
size

## Slide 65: Opportunities and Challenges
(euphemism for problems)

## Slide 66: The 4 Determinants of Time Resolution
  Signal/Noise (S/N)
  Analog Band-width (ABW)
  Sampling Rate
  Signal statistics
J.F. Genat, F. Tang, H. Frisch, and G. Varner; Picosecond Resolution Timing Measurements, Nucl. Instr. Meth A607, 387 (2009);
Workshop on The Factors that Limit Time Resolution in Photo-detectors, University of Chicago, April 28-29, 2011
5 nsec/div
50 psec/pt

## Slide 67: Simulation of Resolution vs abw
Jean-Francois Genat et al. – Nucl. Inst. Meth. (2009?)
Brown line: 10 Gs/sec (we’ve done >15);
1.5 GHz abw ( we’ve done 1.6); S/N 120 (N=0.75mv, S is app specific)
This (brown) line
This (brown) line
1 ps

## Slide 68: Opportunities:Can we go deep sub-picosec?: the Ritt Parameterization (agrees with JF MC)
S/N, fZ: DONE
abw: NOT YET
100 femtosec
Stefan Ritt slide, doctored

## Slide 69: What’s the limit? (2009 cartoon)
Front Window and Radiator
Photocathode
Pump Gap
High Emissivity Material
Low Emissivity Material
`Normal’ MCP pore material
Gold Anode
50 Ohm Transmission Line
Rogers PC Card
Capacitive Pickup to Sampling Readout
N.B.- this is a `cartoon’- working on workable designs-join us…
Funnel pore with reflection cathode, dynode rings, ceramic anode,…

## Slide 70: Opportunities
Sub psec timing –e.g. Ritt 100 fsec extrp.
Tight pulse height (high SEY 1st strike)
Photocathodes- QE’s >45% (?)
Non-vacuum transfer assembly
Simpler top seal- (incl. metal for neutrons)
Commercialization (SBIR/STTR)

## Slide 71: Current Problems (remember we’re only in 3rd yr)
Uniformity of ALD (parallel efforts at ANL, Arradiance)- will be solved…
Vacuum transfer assembly- ceramic in progress (SSL); >several years for glass package most likely…
`Frugal’ top seal for glass package (progress)
Optimization for specific applications (e.g. Collider, KOTO, HE and LE neutrinos, PET
Lack of simulation for applications (help?)

## Slide 72: More Information on LAPPD:
Main Page: http://psec.uchicago.edu (has the links to the Library and Blogs)
Library: Workshops, Godparent Reviews, Image Library, Document Library, Links to MCP, Photocathode, Materials Literature, etc.;
Blog: Our log-book- open to all (say yes to certificate Cerberus, etc.)- can keep track of us (at least several companies do);

## Slide 73: The End
oy- chemistry

## Slide 74: Backup slides

## Slide 75: Backup: Motivation

## Slide 76: Medical Imaging- TOFPET
PET slides from Bill Moses’s talk at the Clermont Workshop (see http:hep.uchicago.edu/psec)
TOF adds 3rd dimension to Positron-Emission Tomography
Clinical flat-bed scanner?
Low-density multi-layer sampling gamma detectors?
Cheap robust electronics
Real-time imaging?
Lower Dose rate

## Slide 77: What sets the 1 psec goal for HEP?

## Slide 78: KL to pizero nu-nubar

## Slide 79: Applications
SRI’s NABC Approach http: //www.itu.dk/~jeppeh/DIKP/NABC.pdf (sic- Denmark?)

## Slide 80: Sampling calorimeters based on thin cheap photodetectors with correlated time and space waveform sampling
Proposal: Alternating radiator and cheap 30-50 psec thin planar mcp-pmt’s on each side (needs simulation work)
    Bill Moses (Lyon)

## Slide 81: Application 4- Cherenkov-sensitive Sampling Calorimeters
A picture of an em shower in a cloud-chamber with ½” Pb plates (Rossi, p215- from CY Chao)
A `cartoon’ of a fixed target geometry such as for JPARC’s KL-> pizero nunubar (at UC, Yao Wah) or LHCb
I
Idea: planes on one side read both Cherenkov and scintillation light- on other only scintillation.

## Slide 82: Backup: MCP’s and Assembly

## Slide 83: Demonstration of The Internal ALD HV Divider in the Demountable
Demountable at APS

## Slide 84: Hermetic Packaging
Top Seal and Photocathode- this year’s priority
Commercial RFI for 100 tiles
(Have had one proposal for 7K- 21K tiles/yr)
Tile Development Facility at ANL
Production Facility at SSL/UCB
3 parallel paths

## Slide 85: Micro-Channel Plate Development
Incom with SSL testing developed 8”-sq high-quality MCP Plates
Characterization of SEY of emitting materials (ANL/MSD, here for Arradiance)
Detailed simulation of MCP’s and materials; comparison with data
Incom 8”-sq high-quality MCP plate with > 65% OAR

## Slide 86: A `Quasi-digital’ MCP-based Calorimeter
Electron pattern (not a picture of the plate!)- SSL test, Incom substrate, Arradiance ALD. Note you can see the multi’s in both plates => ~50 micron resolution
Note- at high gain the boundaries of the multi’s go away
Idea: can one saturate pores in the the MCP plate s.t.output is proportional to number of pores. Transmission line readout gives a cheap way to sample the whole lane with pulse height and time- get energy flow.
Oswald Siegmund, Jason McPhate, Sharon Jelinsky, SSL (UCB)

## Slide 87: MCP+Transmission Lines Sampled at Both Ends Provide Time and 2D Space
8” Tiles
10-15 GS/sec Waveform Sampling ASICS
Field Programable Gate Arrays
(not as shown- PC cards will be folded behind the panel- not this ugly…
Single serial Gbit connection will come out of panel with time and positions from center of back of panel

## Slide 88: Micro-channel Plates PMTs
Satisfies small feature size and homogeneity
Photon and electron paths are short- few mm to microns=>fast, uniform Planar geometry=>scalable to large areas

## Slide 89: ALD for Emissive Coating
89
Many material possibilities
Tune SEE along pore (HF- possible discrete dynode structure (speed!)
Conventional MCP’s:
Alternative ALD Coatings:
(ALD SiO2 also)
Jeff Elam , Zeke Insepov, Slade Jokela
Notes: 89

## Slide 91: Backup: Testing

## Slide 92: Micro-Channel Plate Performance
ALD plates show no aging
Gains are as good or better than commercial
Noise is <0.1 cts/cm2-sec (very good)
Pulses from two ALD-functionalized MCP’s measured on 2 ends of an 8” anode RF strip
SSL
SSL
SSL
ANL

## Slide 93: LAPPD Performance
Fast Preconditioning
Low noise
400 micron resolution
(8” plate, anode, PSEC-4)
High Gain (>107)

## Slide 94: First measurements of gain in an ALD SEE layer at the APS laser test setup (Bernhard Adams, Matthieu Cholet, and Matt Wetstein)
Testing Group: Bernhard Adams, Matthieu Cholet, and Matt Wetstein at the APS, Ossy Siegmund’s group at SSL
LAPPD Preliminary
(very)
MCP and Photocathode Testing
N. B.!

## Slide 95: Backup: Electronics

## Slide 96: Electronics- Integration & Performance
Eric Oberla and Craig Harabedian cabling SuMo digital and central FPGA cards
Analog Bandwidth of strip-line anode
Time resolution on 2 ends of anode strip vs (S/N)-1 in psec
PSEC-4 sampling at 13.3 Gsamples/sec with > 65% OAR
This is the `money’ plot

## Slide 97: FY-08 Funds –Chicago Anode Design and Simulation (Fukun Tang)

## Slide 98: Front-end Electronics/Readout Waveform sampling ASIC
First have to understand signal and noise in the frequency domain
Electronics Group: Jean-Francois Genat, Gary Varner, Mircea Bogdan, Michael Baumer, Michael Cooney, Zhongtian Dai, Herve Grabas, Mary Heintz, James Kennedy, Sam Meehan, Kurtis Nishimura, Eric Oberla, Larry Ruckman, Fukun Tang
A typical MCP signal (Planacon)
Frequency spectra of signal and noise (JF Genat)

## Slide 99: Backup: Photocathodes

## Slide 100: Achievements: PhotoCathodes
Have made >20% 8”PC at SSL; 25% small PC’s at ANL, 18% 4” (larger underway)
SSL 8” SbNaK cathode
4” cathode: Chalice in Burle oven
QE of SSL 8” SbNaK cathode
QE of ANL small SbKCs cathodes
ANL
ANL

## Slide 101: Backup: Miscellaneous

## Slide 102
Fabricated per unit cost estimates
30 1000 3000 10,000 100,000
Window (1@) $18 13 11 10 8
Side wall (1@) $78 55 52 48 40
Base plate (1@) $20 13 11 10 8
Rod Spacers (75@) $7 3 2 1.20 .80
Total $641 $306 $224 $158 $116
The above prices are for water jet cut B33 glass, tol. +- 0.010, except rod spacers +000 -0.004
---------Quotations--------- -----------------------Cost estimates----------------------
8” Glass Package Component Costs
To this add 2 8” plates (@250?), ALD (Bulk), PC, assembly
Rich Northrop

## Slide 103: Detector Development- 3 Prongs
MCP development- use modern fabrication processes to control emissivities, resistivities, out-gassing
Use Atomic Layer Deposition for emissive material
(amplification) on cheap inert substrates (glass capillary arrays, AAO). Scalable to large sizes; economical; pure – i.e. chemically robust and (it seems- see below) stable
Readout: Use transmission lines and modern chip technologies for high speed cheap low-power high-density readout.
Anode is a 50-ohm stripline. Scalable up to many feet in length ; readout 2 ends; CMOS sampling onto capacitors- fast, cheap, low-power (New idea- make MCP-PMT tiles on single PC-card readout- see below)
Use computational advances -simulation as basis for design
    Modern computing tools allow simulation at level of basic processes- validate with data. Use for `rational design’ (Klaus Attenkofer’s phrase).

## Slide 104: The Large-Area Psec Photo-Detector Collaboration-2010

## Slide 105
Distinguishable only by mass (and possibly lifetime)- hence measure velocity (v) and momentum (gmv) of the parent particle to find out m and thus the quark content.
Nico Berry (nicoberry.com)
Charge +2/3e
The bizarre structure of basic matter
M=175,000 MeV
M=4,500 MeV
M~2 MeV
M=1750 MeV
M=300 MeV
Charge -1/3e