## Slide 1: Development of Bialkali Transfer Photocathodes for Large Area Micro-Channel Plate Based Photo Detectors
1Argonne National Laboratory, Argonne, IL
2University of Chicago, Chicago, IL
3Fermi National Accelerator Laboratory, Batavia, IL
Junqi Xie1, Marcel W. Demarteau1, Henry J. Frisch1,2, Joe Gregar1, Richard Northrop2, Alexander Paramonov1, Anatoly Ronzhin3, Greg Sellberg3, Robert G. Wagner1, Dean Walters1, Zikri Yusof1
On behalf of LAPPD Collaboration

## Slide 2: Outline
Motivation
Small PMT Photocathode Growth and Characterization
Large Area Photocathode Growth and Characterization
Summary
Future Work

## Slide 3
Motivation: LAPPD Approach
3
61 cm
41 cm
PMT
LAPPD

## Slide 4
Incoming photon
Glass Window
Photocathode
MCP1
Anode signal generation
MCP2
Many fundamental detector properties such as dark current, quantum efficiency, response time, and lifetime are determined by the properties of the photocathode.
Motivation: Photocathode
Photocathode:
Convertion of photons to electrons

## Slide 5: Resource: Infrastructure
Basic Sciences Program
  Growth and Characterization Facility
  General Lab-Infrastructure
  User facility use
    APS
    NSLS
    Nano center BNL/ANL
Large Area Development
  Growth Equipment
  Source Development Infrastructure
Microscopic Property
Macroscopic Property
Industrial Fabrication
Production Unit
(8’’X8’’) (not yet existing)
  Test Facility for Recipe optimization (industrial standard)
  Detector integration Facility

## Slide 6: In-Situ Structural and Chemical Characterization In-situ X-ray Scattering (by K. Attenkofer and S. Lee)
Macroscopic film properties
  Film thickness
  Roughness
Microscopic composition
  Which phases are present
  Lateral and transversal and homogenuity
  Crystalline size
  Preferential crystal growth
Surface composition
  Local workfunction
  Chemical composition
Movie like characterization during the growth:
An Sb phase transition was observed from amorphous to crystalline at 7~8 nm by XRD.
In-situ Sb layer growth and K inter-diffusion process were monitored by real-time XRR.

## Slide 7: Small PMT Photocathode Growth Process
Oxygen discharge cleaning and oxidation;
Sb deposition monitoring via reflectivity measurement;
Bake out temperature, deposition temperature;
Control of alkali metals deposition.
Apply these to the fabrication of
large area photocathode.

## Slide 8
Commissioning of Optical Station
Movable optical station can be used for both in situ and ex situ optical and electrical measurements.
QE measurement by Hamamatsu and ANL optical station agree well with each other indicating the home-built optical station is reliable.

## Slide 9
Small PMT Photocathode Characterization
QE Measurement
I-V Characteristic
Cathodes exhibit characteristic I-V behavior, with QE as high as 24% at 370 nm.
The quick drop at short wavelength is due to glass absorption.

## Slide 10: The Chalice Design
Design is based on the small PMT tube, the chalice can be seen as a LARGE PMT tube.
Top glass plate is replaceable for reuse.
Chalice structure is supported by external legs.
An X-Y scanner was designed and built for QE scan.

## Slide 11: Sb Beads Arrangements for the Chalice
Numerical simulation of Sb thickness as a function of Sb beads arrangements and distance from window;
4 Sb beads arrangement
2.5” distance from the window;
This arrangement produces sufficient uniformity on a 4”x4” window as our starting point;
This assumes all the beads perform identically.

## Slide 12
Chalice Photocathode Characterization
QE Measurement
I-V Characteristic
Plasma was not performed properly, due to low plasma power supply.

## Slide 13
Chalice Photocathode Deposition
The QE mapping is obtained at 350 nm wavelength, scan step size: 0.2 inch
Sb bead
QE Scale
The blue area is the 4’’X4’’ window edge.
QE is uniform (15%) at a large area.

## Slide 14
Sb bead
Center X: Lighting rod, which affect the Sb film deposition
X
X
Comparison of QE Map and Sb Transmission Map
1 bead
4 beads
QE Map
Sb Film Transmission Map

## Slide 15
Sb Film Transmission Curve with Different Photocathode QE
Film transmission with known QE were measured and plotted.
Film transmission increases as wavelength increases without regarding the QE value
The film transmission values at 400 nm were chosen to plot the relation between KCs-Sb cathode QE and film transmission.
The highest QE is around 78% Sb transmission (400nm beam).

## Slide 16: Summary
Photocathode growth and characterization instruments were set up.
PMT photocathodes with QE as high as 24% have been produced.
Large area (4’’X4’’) photocathode with uniform QE (15%) were achieved even without proper oxygen plasma cleaning and oxidation.
All photocathodes show typical I-V characteristics.
QE of the photocathode is related to base Sb layer thickness.
The optimized Sb thickness for KCs-Sb photocathode is around 78% transmission (400nm beam).
Next Steps
Work out the plasma configuration to obtain uniform photocathode.
Complete absolute reflection measurement of Sb films and relate to the film transmission data.
Study the effect of plasma cleaning and oxidation to the photocathode QE.
Optimize the process for higher QE cathode based on the micro and macro studies.

## Slide 17
Back Up

## Slide 18
Relation between Cathode QE and Sb Film Transmission
Relate the QE of the KCs-Sb cathodes with the Sb film transmission at 400 nm.
KCs-Sb Photocathode
Cs-Sb Photocathode
Note that the highest QE is around 78% Sb transmission (400nm beam), similar to that of Cs-Sb cathode at around 82% Sb transmission (blue light) as reported.
MARTIN ROME, J. Appl. Phys, 26, 166, 1955